|  | Materials & Metallurgy Group |  | CRM/MS/01 |
| --- | --- | --- | --- |
|  | Material Specification | 817M40 (EN24) |  |

## 1. SCOPE

This standard prescribes the specifications and technical supply conditions of steel 817M40 (EN24). The conditions prescribed here are required to be satisfied by the supplier.

## 2. SPECIFICATIONS

| Code | 817M40 |
| --- | --- |
| Colour | Not specified |
| Equivalent Specs | 40Ni6Cr4Mo3, 817M40 (EN24), 36CrNiMo4, SNCM8, 4340, IS : 11185, PD 970-2005, DIN, JIS, AISI |
| Standards | IS 2853, ASTM E112, AS 4163, ASTM E45, IS ASTM E407, IS:11371, IS:6396, IS:11185 |

## 3. CHEMICAL COMPOSITION

| Element | C | Si | Mn | P | S | Ni | Mo | Others |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Min | 0.36 | 0.10 | 0.45 | Not specified | Not specified | 1.30 | 0.20 | Not specified |
| Max | 0.44 | 0.35 | 0.70 | 0.035 | 0.035 | 1.70 | 0.35 | Not specified |

## 4. MECHANICAL PROPERTIES

| Property | Min | Max | Unit |
| --- | --- | --- | --- |
| Hardness (HB) | 180 | 230 | HB |

## 5. METALLURGICAL PROPERTIES

Grain Size: 5-8

Inclusion Rating: Thin Series / Thick Series (AS 4163/ASTM E45)

Microstructure: Uniformly Distributed ferrite & pearlite, banding limit 0.050 mm

Surface Condition: Black

Heat Treatment: Annealed / Normalized as hot rolled or forged

Source Pages: [1]